Addition of Local Buckling Ratio and Torsional Constant as a Sectional Property for Parallel Bearing Piles (PBP) Sections in IS 12778:2004

Shubham Dashore1, Dolendra Patel2

2Assistant Professor

Shri Shankaracharya Institute of Engineering and Technology, Bhilai, India, 49100

Abstract – Generally all the structural steel products are essential for construction purposes, as they help in designing and building industrial and warehouse spaces. Structural steel is known for its shear strength, hardness, durability and more. In addition, this metal can easily absorb shocks, due to which most residential, industrial, and commercial buildings are constructed with structural steel. The sectional properties of hot rolled parallel flange steel sections listed in IS 12778:2004 for PBP sections include Moment of Inertia, Radius of Gyration, Elastic Section Modulus and Plastic Section Modulus; each about the major and minor axes which is generally required from design point of view. Few other properties which are frequently required while designing by limit state method and can be added in IS 12778:2004 are the local buckling ratio and the torsional constant.

INTRODUCTION

According to the IS 12778:2004, covering the nominal dimensions, mass and sectional properties of hot rolled parallel flange beams, columns and bearing piles, the pile sections are classified as parallel flange bearing piles. These parallel flange bearing piles, generally known as PBP, is the type of IS Parallel Flange Sections, in which flanges and webs are of same thickness and nominal depth and nominal flange width are also same. Accordingly, PBP sections are designated by nominal depth and mass of the section in kg/m. For example, a section PBP 300 x 150.00 would mean that the bearing pile section having nominal depth of 300 mm, nominal flange width of 300 mm and a mass of 150.00 kg/m. They are doubly symmetric wide flange shapes and are generally used as bearing piles. The bearing piles are used for compression members. The load carrying capacities of parallel flange sections under direct

compressions are much higher than that of sections available today. Also the connections to the flanges are easier and simpler since no tapered washers, etc. are required.

Fig.1 Parallel Bearing Piles

METHOLOGY

The shear center is the point through which the applied loads must pass to produce bending without twisting. If a shape has a line of symmetry, the shear center will always lie on that line; for cross-sections with two lines of symmetry, the shear center is at the intersection of those lines (as is the centroid). The torsional constant, also known as the St. Venants torsional constant, occurs due to the torsional restraint in which the cross-section is prevented from rotation about the shear centre.

The stability of a flexural member is very often a function of its torsional stiffness. One of the assumption made in the theory of torsion is that a plane section remain plane after twisting, which is true for round shapes only. It is because no warping exists on a circular cross-section and the entire torque is transferred entirely by the shear. However, the steel beam sections are normally open non circular thin walled sections. For such sections torsional rigidity is much less than flexural rigidity.

The nature of buckling process for an ideal beam is same as that of an ideal column. This implies that the beam is stable with no tendency of lateral-torsional buckling until the bending moments reaches a certain critical magnitude Mcr, whereupon the beam becomes unstable and undergoes rotations and deflections of any magnitude, leading to collapse. The torsional behavior of the structural steel shapes is different and is described by two phenomena:- St.Venant torsion and warping torsion. From the elastic stability theory, the expression for the stability limit state, for a steel beam applied with uniform moment, the critical moment Mcr is given by:-

where, EIy = flexural rigidity (minor axis)

GIt = torsional rigidity

It, Iw = torsion constant and warping constant.

L = unbraced length of the beam subjected to constant moment in the plane.

The above equation for calculating the elastic critical moment corresponding to lateral torsional buckling of a doubly symmetric torsionally restrained prismatic beam subjected to uniform moment in the unsupported length can be simplified and given as :-

where, Iy, Iw, It = moment of inertia about the minor axis, warping constant and torsional constant, respectively.

G = modulus of rigidity

LLT = effective length against lateral-torsional      buckling

The Torsional constant is given by :-

where,

and ,

Most of the structural members are made economical by placing most of it away from the centroidal axis and by making the elements thin. But such members may buckle locally out of their original plane under compression. Local buckling adversely affects the load carrying capacity of columns and beams due to reduced stiffness and strength of the locally buckled plate elements of the section.

For an I-Section beam, the compression flange undergoes local buckling, whereas web being partially in compression and partially in tension, buckles as a plate subjected to in-plane bending. The local buckling generally may occur in the region of maximum bending moment only. The local buckling can be prevented by controlling the width-to-thickness ratio or by adopting higher thickness of the elements.

Depending on the cross section elements such as b, d, D, tw and tf, the local buckling can be found by using the formulas :-

For flange:-

For web:-

where,

bf = width of the flange.

tf = thickness of the flange.

tw = thickness of the web.

The Local buckling ratio is generally used to classify the section under 4 categories as:-

- Plastic (Class 1) if the section satisfies the condition (.

- Compact (Class 2) if the section satisfies the condition (

- Semi-compact (Class 3) if the section satisfies the condition

- Slender (Class 4) if the section satisfies the condition (

Depending upon the cross-section of different PBP sections falling under different classes, the section can be governed as the most critical section.

CONCLUSION

These sections are more efficient in terms of strength, workability and economy. Uses of such sections are increasing in India, nowadays, mostly because they have a greater resistance against pure bending.

Addition of properties such as warping constant and local buckling ratio for flange and web is suggested either in IS 12778:2004 or elsewhere for ready reference because these properties are frequently required while designing by limit state method and are presented here. Addition of these properties will make it easier and simpler for the practicing designers and budding engineers as these will be readily available for them for designing.

A majority of PBP sections are classified as Class 2 Compact or better when in pure bending. They can therefore attain their full plastic moment capacity. Also, a majority of sections are classified as Class 3 Semi-Compact or better when loaded upto its maximum capacity. The whole cross-section of these sections is therefore effective. The remaining sections may behave as Class 3 Semi-Compact, if subjected to relatively smaller axial loads instead of loading them to their maximum capacity. No PBP section, except PBP 360 x 83.44, is classified as Class 4 Slender under pure bending.

REFERENCES

- Draft IS 800, “Code of Practice for General Construction in Steel (Third Revision)”, Bureau of Indian Standards, New Delhi, India, October 2004.

- N. Subramanium, “Design of Steel Structures – Limit State Method”, ”Oxford publication”,2018

- IS 12778 : 2004, “Hot Rolled Parallel flange Steel sections for Beams, Columns, and Bearing Piles – Dimensions and Section Properties (First revision)”, Bureau of Indian Standards, New Delhi, September 2004.

- S.S. Bhavikatti, “Design of Steel Structure”, by Limit State Method as per IS 800:2007, Fifth Edition, September 2017.

- IS 2062 : 1999, “Steel for General Structural Purposes”, Bureau of Indian Standards, New Delhi, India.

- IS 800 : 1984, “Code of Practice for General Construction in Steel (Second Revision)”, Bureau of Indian Standards, New Delhi, India.

- IS 8500 : 1991, “Structural Steel – Micro alloyed (Medium and High Strength Qualities)”, Bureau of Indian Standards, New Delhi, India.

- S.K. Duggal, “Limit State Design of Steel Structures”, Second Edition, Tata McGraw Hill Publication, 2014.

- Seaburg, P.A., and Carter, C. J., “Torsional Analysis of Structural Steel Members”, Steel Design Guide Series No. 9, Second Printing, American Institute of Steel Construction, Chicago, Illinois, October 2003.

- SteelUK - Dimensions and Properties of UK structural Steel shapes, Techno Consultants Ltd., Manchester, England, November 2000.

- Himanshu Gaur, “Optimization of Sectional Dimensions of I-Section Flange Beams and Recommendations for IS 808: 1989”,  Kota, India, 31st March 2016.

- Keith M. Mueller, “Torsional Analysis of Steel Sections”, American Institute of Steel Construction, Chicago, 2002.

Table 1: Additional Sectional Properties of Parallel Flange Bearing Piles (PBP) Sections

Table 1 (Contd.) : Additional Sectional Properties of Parallel Flange Bearing Piles (PBP) Sections